Nekatere mehanske lastnosti izbranih kamnin:

The uniaxial compressive strength, C0, loading Young's modulus, E,
and Poisson's ratio, , for a number of rocks.
Rock	C0 / (kpsi)	E / (106 psi)	 
Granite, Westerly	33.2	8.1
Quartzite, Cheshire	66.7	11.4	0.11
Diabase, Frederick	70.6	14.4
Marble, Tennessee	22.1	6.9
Granite, Charcoal	25.1	6.4
Shale, Witwatersrand	24.9	9.8	0.23
Granite Aplite (Cheri)	85.2	12.0	0.20
Quartzite, Witwatersrand	29.0	11.3
Dolerite, Karroo	48.0	12.2
Marble, Wombeyan	11.2	9.4
Sandstone, Gosford	5.36	1.4
Limestone, Solenhofen	32.5	7.7

Note: 1 psi = 6895 Pa, 1 kpsi = 1000 psi

Vir: Jaeger J.C., Cook N.G.: Fundamentals of Rock Mechanics,
Methuen & Co LTD, London, 1969.

TABLE VIII. Elastic and Strength Properties of Some Rocks and metals
Rock or metal	E x 10-5 / kg/cm2	 /  / 	Ultimate / compressive / strength, / kg/cm2	Ultimate / tensile / strength, / kg/cm2	Ultimate / shear / strength, / kg/cm2
Amphibolite	6.3	0.28-0.3	1,700-2,800	90-120
Argillite	3.2	0.3	450-1,200	—
Basalt	9.0-12.0	0.24	300-400	—	175-460
Gabbro	10.7	0.31	3,100	—
Granite	5.0-9.0	0.10-0.31	1,000-2,500	100-150	100-300
Limestone	4.0-7.0	0.19-0.22	900-1,200	120	180
Quartzite	4-10	0.15-0.19	2,900-3,000	108-150	150-207
Marble	6.0-9.0	0.34-0.40	600-1,900	60-160	240-310
Sandstone	0.5-5	0.19-0.21	350-1,500	30-100	230
Quartzitic sandstone	3-4	0.09	1,200-2,000	30-120	—
Arkosic sandstone	5	0.13	1,300	30	—
Martite hornfels	8	—	2,900-3,000	30-90	—
Quartz-sericitic schist	1.2-3	0.16	670	70
Coal	3.6-6.0	0.14-0.16	200-500	15-25	90
Aluminium	7.2	0.34		900-1,200
Iron	26.7	0.28		2,900‑4,500
Copper	12.5	0.35		1,500‑2,000
Lead	1.66	0.45		120-200

Vir: Rzhevsky V., Novik G.: The Physics of Rock, MIR Publishers, Moscow, 1971

TABLE IX.	Anisotropy of Mechanical Properties of Some Rocks

Rock	Young's modulus / E×10-5 kg/cm2		Poisson's ratio		Ultimate compressive strength, / kg/cm2
	=		=		=	
Sandy shales	3.03	2.42	0.25	0.16	518	789
Limestones	6.36	7.25	0.28	0.30	1,510	1,250
Anthracites	0.42	0.54		0.13	105	160
Coarse-grained / sandstones	1.93	1.73	0.45	0.36	1,185	1,423
Fine-grained / sandstones	3.83	2.64	0.20	0.19	1,597	1,568
Siltstones	2.67	1.72	0.25	0.29	506	675
Brown coal					101	235

Note:	= parallel to the stratification
 perpendicular to the stratification

Vir: Rzhevsky V., Novik G.: The Physics of Rock, MIR Publishers, Moscow, 1971

TABLE X. Static and Dynamic Elastic Properties of Some Rocks
Rock	Static modulus of elasticity / Estat×10-5 kg/cm2	Dynamic modulus of elasticity / Edyn×10-5 kg/cm2	Ratio / Edyn/Estat	Bulk / modulus / K×10-5 kg/cm2	Rigidity or / shear modulus / G×10-5 kg/cm2
Sandstone with / chalcedonic cement	7.30	7.78	1.07	2.30	3.20
Equigranular dolomite	5.05	5.31	1.00	5.21	1.88
Limestone	1.88	2.42	1.29	4.35	0.66
Calcareous dolomite	3.49	4.72	1.35	3.70	1.30
Fine-grained detrital limestone	4.77	5.71	1.20	4.60	1.80
Granite	6.60	7.10	1.08	4.73	2.60
Gabbro	7.10	7.50	1.06	5.70	3.60
Dunite	14.90	16.40	1.03	10.73	5.90
Syenite	7.40	8.10	1.10	5.40	2.90

Vir: Rzhevsky V., Novik G.: The Physics of Rock, MIR Publishers, Moscow, 1971

TABLE XI. Angles of Internal Friction, Cohesion and Looseness Factor of Some Rocks

Rock	Angle of internal friction, degrees	Cohesion, / kg/cm2	Looseness / factor
Sand	32	0.9-5	1.05-1.2
Fat clay	20	0.85-3.3	1.2-1.25
Argillite	30	0.4-30.0	1.2-1.3
Brown coal	36	12-35.0	1.2-1.4
Hard rocks	45-60	up to 200-300	1.8-2.5

Vir: Rzhevsky V., Novik G.: The Physics of Rock, MIR Publishers, Moscow, 1971